## Slide 1: Group Discussion 2 – Cheaper coke to reduce aluminum production cost ? Presentation
Choice between 2 options
  Existing coke (coke E)
  Blend : 2/3 coke E + 1/3 coke A
Coke A characteristics
  50 $/t cheaper
  High air reactivity
Pilot anodes have been produced with the blend
  Gives the key properties of the potential new anodes

## Slide 2: Group Discussion 2 – Cheaper coke to reduce aluminum production cost ? Potential gains
Coke A required = 1/3 x 360 = 120 kg/tAl
Expected gain = 0.12 x 50 = 6 $/tAl
Pitch = 90 kg/tAl
Coke = 360 kg/tAl
Butts = 140 kg/tAl
Anodes = 560 kg/tAl
NCC = 420 kgC/tAl

## Slide 3: Group Discussion 2 – Cheaper coke to reduce aluminum production cost ? Potential loss
Decrease in the anode quality  Increase of the Net Carbon Consumption
Fisher formula : link between anode properties and NCC
Blend anode additional NCC = 20.8 kgC/tAl
Anode price = 600$/kganode
Financial summary
  Gain : 6 $/tAl
  Loss : 600 x 0.02 = 12 $/tAl
  Balance : - 6 $/tAl
NO GO !

## Slide 4: Group Discussion 2 – Cheaper coke to reduce aluminum production cost ? Improved baking
Increase the baking temperature to 1150°C to reduce the air reactivity.
  4% gain on air reactivity residue
  Slight reduction of CO2 reactivity
  Increase of thermal conductivity
New Blend anode additional NCC = 13 kgC/tAl
Additional consumption
  1 liter oil ≈ 1 Nm3 gas ≈ 10 kWh ≈ 0.5 to 1 $
  + 50°C Tbaking  10% consumption increase
  Baking consumption : 2 GJ/tanode And 0.56 tanode/tAl
  Financial impact : 1.6 to 3.2 $/tAl
Financial summary
  Gain : 6 $/tAl
  Carbon Loss : 600 x 0.013 = 7.8 $/tAl
  Baking loss : 1.6 to 3.2 $/tAl
  Balance : - 3.4 to -5 $/tAl
NO GO

## Slide 5: Group Discussion 2 – Cheaper coke to reduce aluminum production cost ? Current Efficiency Loss
What about a current efficiency loss of 1% ?
Loss of production of 0.01 tAl
0.01 t x (2200 $/t – 2x400 $/t) = 14 $/tAl
Financial summary
  Gain : 6 $/tAl
  Carbon Loss : 600 x 0.02 = 12 $/tAl
  CE loss = 14 $/tAl
  Balance : - 20 $/tAl