## Slide 1: Group discussion II
Increased Energy Consumption due to Elevated Anode Resistivity

## Slide 2: What is the impact of the elevated anode resistivity on the energy consumption and accordingly the smelter cost
Anode height = 650mm. Stub hole = 100mm.
Estimate 25% butt height of anode height.
Average height of anodes in pots due to consumption estimate:
  (600mm + 100mm)/2 = 350mm = L
 = 63 – 53 = 10 m
 = R*A/L
U = I*R = I/A * * L = 0,8 * 10^4 A/m2 * 10m* 0,350m = 2,8*10^-2 V= 0,028V
E = 2,98 * U /CE = 2,98 * 0,028V/0,945 = 0,09MWh/t
Cost = 0,09MWh/t * 500000t * 60$/MWh = 2,7M$/a

## Slide 3: What are the potential root causes for this elevated anode resistivity? (1 of 2)
Root causes are porosity and internal cracks increasing the resistivity.
All root causes should be investigated one by one. Find appropropriate solutions that compensate for the below issues.
1. Baking
  Baking temp too low
  Soaking time too low
  Heat up rate too high in the critical temp area (internal cracks)
2. Green anodes
  Pitch content not optimal
  Fines (blaines) proportion not correct
  Butt % and butt properties
  Dry Aggregate recipe
  Green scrap quality
  Green anode handling (internal cracks)

## Slide 4: What are the potential root causes for this elevated anode resistivity? (2 of 2)
3. Raw materials
  Coke:
    Specific Electrical resistivity of calcined petroleum coke
    Calcination temp or time not optimal (real density)
    Bulk density not optimal
    Shipment variations
    Segregation due to storing of coke in piles
  Coal tar pitch
    QI content not optimal
  Butts
    Low quality (soft/density)